NSP 	    Pearlized Sealable Film

PRODUCT OVERVIEW 
NSP is a coextruded BOPP film specially designed for food packaging and lamination applications. It combines excellent opacity and whiteness with good dead-fold properties, high stiffness, and mechanical strength. The film also provides a wide sealing range and a glossy, high-quality surface, making it suitable for high-quality rotogravure and flexographic printing.

KEY FEATURES

- Very good opacity and whiteness

- Excellent web flatness

- Very good dead-fold properties

- Wide sealing range

- Excellent glossy surface

- High mechanical strength and stiffness

APPLICATIONS

- General-purpose food packaging

- Lamination applications

- High-quality rotogravure printing

- Flexographic printing

TECHNICAL DATA — TYPICAL VALUES

| Property |  | Unit | Typical values |  |  |  |  |  |  | Test Method |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Thickness |  | µm | 25 | 30 |  | 35 |  | 40 |  | NODA PLAST Lab |
| Unit Weight |  | g/m² | 17 | 20.4 |  | 23.28 |  | 27.2 |  | NODA PLAST Lab |
| Yield |  | m²/kg | 58.8 | 49 |  | 42 |  | 36.8 |  | NODA PLAST Lab |
| Density |  | g/cm3 | 0.68 |  |  |  |  |  |  |  |
| Wetting Tension |  | mN/m | ≥ 38 |  |  |  |  |  |  | ASTM D2578 |
| Whiteness Index |  | — | 89 |  | 90 |  | 90 |  | 92 | — |
| Opacity |  | % | 70 |  | 72 |  | 73 |  | 76 | DIN 53146 |
| Gloss |  | — | 90 |  | 90 |  | 93 |  | 97 | ASTM D2457 |
| COF Dynamic F-F (U-U) |  | — | ≤ 0.30 |  |  |  |  |  |  | DIN EN ISO 8295 |
| Tensile Strength | MD | MPa | 103 |  |  |  |  |  |  | ASTM D882 |
|  | TD |  | 141 |  |  |  |  |  |  | ASTM D882 |
| Elongation at Break | MD | % | 140 |  |  |  |  |  |  | ASTM D882 |
|  | TD |  | 32 |  |  |  |  |  |  | ASTM D882 |
| Tensile modulus of elasticity | MD | MPa | 1050 |  |  |  |  |  |  | ASTM D 882 |
|  | TD |  | 1980 |  |  |  |  |  |  | ASTM D 882 |

TECHNICAL NOTES

The numerical values reported in this data sheet are obtained from the average of the values recorded in our laboratory tests. Before final use, we recommend technical tests to ensure the film's suitability for the intended use. NODA PLAST Film is not responsible for inappropriate use of the product, and its liability is limited to the exclusive replacement of the product, excluding any compensation or damages of any kind.