NLV 	LABEL VOIDED FILM

PRODUCT OVERVIEW
NLV is a coextruded BOPP film with a micro-voided core structure, developed as a lightweight substrate for label and packaging applications. The film combines a multilayer construction with a controlled surface structure to provide consistent performance during converting.

KEY FEATURES

- High opacity and whiteness

- Excellent web flatness

- High gloss on treated surface

- Rotogravure & flexographic printing

- High mechanical properties

- High stiffness

APPLICATIONS

- Wrap-Around Labels

- Over-Wrap

- Bottle & Container Labels

- Food & Beverage Labels

- Household Product Labels

- Personal Care Labels

TECHNICAL DATA — TYPICAL VALUES

| Property |  | Unit | Typical values |  | Test Method |
| --- | --- | --- | --- | --- | --- |
| Thickness |  | µm | 38 | 47 | NODA PLAST Lab |
| Unit Weight |  | g/m² | 23.6 | 32 | NODA PLAST Lab |
| Yield |  | m²/kg | 42.4 | 31.25 | NODA PLAST Lab |
| Density |  | g/cm³ | 0.68 |  | — |
| Wetting Tension |  | mN/m | ≥ 38 |  | ASTM D2578 |
| Whiteness Index |  | — | 90 | 92 | — |
| Opacity |  | % | 81 | 83 | DIN 53146 |
| Gloss |  | — | 90 | 90 | ASTM D2457 |
| COF Dynamic F-F (U-U) |  | — | ≤ 0.30 |  | DIN EN ISO 8295 |
| Tensile Strength | MD | MPa | 103 |  | ASTM D882 |
|  | TD | MPa | 141 |  | ASTM D882 |
| Elongation at Break | MD | % | 140 |  | ASTM D882 |
|  | TD | % | 32 |  | ASTM D882 |
| Modulus of Elasticity | MD | MPa | 1080 |  | ASTM D882 |
|  | TD | MPa | 2000 |  | ASTM D882 |

TECHNICAL NOTES

The numerical values reported in this data sheet are obtained from the average of the values recorded in our laboratory tests. Before final use, we recommend technical tests to ensure the film's suitability for the intended use. NODA PLAST Film is not responsible for inappropriate use of the product, and its liability is limited to the exclusive replacement of the product, excluding any compensation or damages of any kind.