NSC 	    Transparent Film

PRODUCT OVERVIEW 
NSC is a coextruded, heat-sealable BOPP film designed for food and general-purpose packaging. It offers excellent transparency, gloss, sealing performance, and printability, making it suitable for rotogravure, flexographic printing, and lamination.

KEY FEATURES

- Excellent transparency & gloss

- Wide sealing range

- Good seal strength

- Excellent hot tack

- High mechanical properties & stiffness

- Excellent web flatness

APPLICATIONS

- Food & general packaging

- Lamination

- Rotogravure printing

- Flexographic printing

TECHNICAL DATA — TYPICAL VALUES

| Property |  | Unit | Typical values |  |  |  |  |  |  | Test Method |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Thickness |  | µm | 20 | 25 |  | 30 |  | 40 |  | NODA PLAST Lab |
| Unit Weight |  | g/m² | 18.2 | 22.7 |  | 27.3 |  | 36.5 |  | NODA PLAST Lab |
| Yield |  | m²/kg | 55 | 44 |  | 36.6 |  | 27.4 |  | NODA PLAST Lab |
| Wetting Tension |  | Dynes/cm | ≥ 38 |  |  |  |  |  |  | ASTM D2578 |
| Haze |  | % | ≤ 3.5 |  | ≤ 3.5 |  | ≤ 3.5 |  | ≤ 3.5 | ASTM D1003 |
| Gloss 45° |  | % | 82 |  | 82 |  | 82 |  | 82 | ASTM D2457 |
| COF Dynamic F-F (U-U) |  | — | ≤ 0.30 |  |  |  |  |  |  | DIN EN ISO 8295 |
| Tensile Strength | MD | MPa | 150 | 140 |  | 140 |  | 140 |  | ASTM D882 |
|  | TD |  | 290 | 290 |  | 290 |  | 290 |  | ASTM D882 |
| Elongation at Break | MD | % | 200 |  |  |  |  |  |  | ASTM D882 |
|  | TD |  | 50 |  |  |  |  |  |  | ASTM D882 |
| Thermal Shrinkage @ 120 °C , 5 min | MD | % | ≤ 5 |  |  |  |  |  |  | NODA PLAST Lab |
|  | TD |  | ≤ 3 |  |  |  |  |  |  | NODA PLAST Lab |
| Heat Seal Range (U-U) |  | °C | 105-140 |  |  |  |  |  |  | NODA PLAST Lab |

TECHNICAL NOTES

The numerical values reported in this data sheet are obtained from the average of the values recorded in our laboratory tests. Before final use, we recommend technical tests to ensure the film's suitability for the intended use. NODA PLAST Film is not responsible for inappropriate use of the product, and its liability is limited to the exclusive replacement of the product, excluding any compensation or damages of any kind.