MATT-S 	    Matt Film (Both Sides Sealable)

PRODUCT OVERVIEW 
Matt-S is coextruded matt BOPP film with one side regular matt sealable layer and other side treated glossy heat sealable layer for good printability.

KEY FEATURES

- xcellent matte dispersion

- Wide sealing range

- Good seal strength

- High mechanical properties

- High stiffness

- Excellent web flatness

APPLICATIONS

- General-purpose packaging

- Lamination applications

- High-quality printed packaging

- Rotogravure printing

- Flexographic printing

TECHNICAL DATA — TYPICAL VALUES

| Property |  | Unit | Typical values |  |  | Test Method |
| --- | --- | --- | --- | --- | --- | --- |
| Thickness |  | µm | 20 | 25 | 30 | NODA PLAST Lab |
| Unit Weight |  | g/m² | 17.6 | 22.2 | 26.7 | NODA PLAST Lab |
| Yield |  | m²/kg | 56.8 | 45.5 | 37.5 | NODA PLAST Lab |
| Wetting Tension |  | mN/m | ≥ 38 |  |  | ASTM D2578 |
| Gloss 45° |  | % | 10 |  |  | ASTM D2457 |
| Haze |  | % | 72 |  |  | ASTM D1003 |
| COF Dynamic F-F (U-U) |  | — | ≤ 0.30 |  |  | DIN EN ISO 8295 |
| Tensile Strength | MD | MPa | 130 |  |  | ASTM D882 |
|  | TD |  | 260 |  |  | ASTM D882 |
| Elongation at Break | MD | % | 150 |  |  | ASTM D882 |
|  | TD |  | 50 |  |  | ASTM D882 |
| Tensile Modulus of Elasticity | MD | MPa | 2000 |  |  | ASTM D882 |
|  | TD |  | 3800 |  |  | ASTM D882 |
| Thermal Shrinkage | MD | % | ≤ 5 |  |  | BMS TT 0.2 |
|  | TD |  | ≤ 3 |  |  | BMS TT 0.2 |
| Seal strength 120°C / 1bar / 1s / flat seals (Untreated-Untreated) |  | N/15mm | > 2 |  |  | BMS TT 0.1 |
| Heat Seal Range (U-U) |  | °C | 125-140 |  |  | Noda-PLAST Lab |

TECHNICAL NOTES

The numerical values reported in this data sheet are obtained from the average of the values recorded in our laboratory tests. Before final use, we recommend technical tests to ensure the film's suitability for the intended use. NODA PLAST Film is not responsible for inappropriate use of the product, and its liability is limited to the exclusive replacement of the product, excluding any compensation or damages of any kind.