NLC 	    Label Clear Film

PRODUCT OVERVIEW 
NLC is coextruded Transparent BOPP film, one side Corona Treated and both sides non-sealable. Film is used for Over wrap and wrap around Labeling.

KEY FEATURES

- Excellent gloss and surface appearance

- Very good machinability

- High mechanical properties

- High stiffness

- Excellent web flatness

- Suitable for high-quality printing

APPLICATIONS

- General-purpose packaging

- General-purpose packaging

- Lamination applications

- High-quality rotogravure printing

- Flexographic printing

TECHNICAL DATA — TYPICAL VALUES

| Property |  | Unit | Typical values |  |  | Test Method |
| --- | --- | --- | --- | --- | --- | --- |
| Thickness |  | µm | 20 | 25 | 30 | NODA PLAST Lab |
| Unit Weight |  | g/m² | 18.2 | 22.7 | 27.3 | NODA PLAST Lab |
| Yield |  | m²/kg | 54.9 | 44 | 36.6 | NODA PLAST Lab |
| Wetting Tension |  | mN/m | ≥ 38 |  |  | ASTM D2578 |
| Opacity |  | % | 1.8 | 2.2 | 2.5 | DIN 53146 |
| Haze |  | % | 1.6 | 1.7 | 1.8 | ASTM D1003 |
| Gloss 45° |  | % | 95 | 94 | 93 | ASTM D2457 |
| COF Dynamic F-F (U-U) |  | — | ≤ 0.30 |  |  | DIN EN ISO 8295 |
| Tensile Strength | MD | MPa | 160 |  |  | ASTM D882 |
|  | TD |  | 290 |  |  | ASTM D882 |
| Elongation at Break | MD | % | 180 |  |  | ASTM D882 |
|  | TD |  | 60 |  |  | ASTM D882 |
| Tensile Modulus of Elasticity | MD | MPa | 2000 |  |  | ASTM D882 |
|  | TD |  | 3800 |  |  | ASTM D882 |
| Thermal Shrinkage | MD | % | ≤ 5 |  |  | BMS TT 0.2 |
|  | TD |  | ≤ 3 |  |  | BMS TT 0.2 |

TECHNICAL NOTES

The numerical values reported in this data sheet are obtained from the average of the values recorded in our laboratory tests. Before final use, we recommend technical tests to ensure the film's suitability for the intended use. NODA PLAST Film is not responsible for inappropriate use of the product, and its liability is limited to the exclusive replacement of the product, excluding any compensation or damages of any kind.