NSMM-M 	    Metallized BOPP Film, One Side C. T

PRODUCT OVERVIEW 
NSMM- M is coextruded BOPP film, one side heat sealable, other side metallized, moderate barrier suitable for food packaging and goods with general use.

KEY FEATURES

- Excellent metal band & homogeneous metal deposition

- Wide sealing range & good seal strength

- Excellent hot tack

- Excellent web flatness

- High mechanical properties & stiffness

APPLICATIONS

- General-purpose packaging

- Lamination

- High-quality rotogravure & flexographic printing

TECHNICAL DATA — TYPICAL VALUES

| Property |  | Unit | Typical values |  |  |  | Test Method |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Thickness |  | µm | 18 | 20 | 25 | 30 | DIN ISO 4593 |
| Unit Weight |  | g/m² | 16.4 | 18.2 | 22.75 | 27.3 | NODA PLAST Lab |
| Yield |  | m²/kg | 60.97 | 54.9 | 43.9 | 36.6 | NODA PLAST Lab |
| Wetting Tension |  | mN/m | ≥ 38 |  |  |  | ASTM D2578 |
| Optical Density |  | — | > 2 |  |  |  | Modus T&D (T= Transmitted light) |
| OTR (23°C-0% RH |  | cc/(m2*day*atm) | < 80 |  |  |  | ASTM D 3985 |
| WVTR (38°C-90% RH) |  | g/(m2*day*atm) | < 0.8 |  |  |  | ASTM F 1249 |
| COF Dynamic F-F (U-U) |  | — | ≤ 0.30 | ≤ 0.31 | ≤ 0.32 | ≤ 0.30 | DIN EN ISO 8295 |
| Tensile Strength | MD | MPa | 150 |  |  |  | ASTM D882 |
|  | TD |  | 290 |  |  |  | ASTM D882 |
| Elongation at Break | MD | % | 180 |  |  |  | ASTM D882 |
|  | TD |  | 60 |  |  |  | ASTM D882 |
| Thermal Shrinkage | MD | % | ≤ 5 |  |  |  | BMS TT 0.2 |
|  | TD |  | ≤ 3 |  |  |  | BMS TT 0.2 |

TECHNICAL NOTES

The numerical values reported in this data sheet are obtained from the average of the values recorded in our laboratory tests. Before final use, we recommend technical tests to ensure the film's suitability for the intended use. NODA PLAST Film is not responsible for inappropriate use of the product, and its liability is limited to the exclusive replacement of the product, excluding any compensation or damages of any kind.